## Slide 1
2026
Changhong Carbon Black
Reinforcing and semi-reinforcing furnace blacks for tires and rubber goods
Zhejiang Changhong Biological Material Co., Ltd.
www.changhongpolymer.com gaoxz@kygroup.ltd
Notes: Hello everyone, and thank you for your time. I am Xuzhe Gao from the carbon black team at Zhejiang Changhong Biological Material. Today I will introduce Changhong Carbon Black: who we are, what makes our carbon black different, our main grades, and how we can start working together.

## Slide 2
Contents
01
Who We Are
02
Why Changhong Carbon Black
03
Product Portfolio
04
Working With Us
Notes: Four parts today. First, a short profile of our company and production bases. Second, why our carbon black is different. Third, the product range, grade by grade. Finally, how a new customer moves from samples to regular supply.

## Slide 3
01
Who We Are
Notes: Let us start with who we are.

## Slide 4: Company Snapshot
Zhejiang Changhong Biological Material Co., Ltd.
The producer behind Changhong Carbon Black
China’s first producer of carbon black made from aromatic-rich oil
Proprietary process removes feedstock impurities — heavy metals not detected
Full range of hard and soft blacks from three bases in Zhejiang and Guangxi
Serving tires, rubber goods, cable and optical-fibre jackets, and plastics modification
3
production bases
Ningbo · Shengzhou · Fangchenggang
350,000 MT
annual capacity in operation
2026
1,000,000 MT
total planned capacity
hard and soft blacks, plus specialty grades
Notes: We are Zhejiang Changhong Biological Material Co., Ltd., the producer behind Changhong Carbon Black. We are China’s first carbon black producer to use aromatic-rich oil as feedstock, and our process removes feedstock impurities, so heavy metals test as not detected. We produce a full range of hard and soft blacks at three bases in Zhejiang and Guangxi, with 350,000 tonnes a year in operation and a total planned capacity of one million tonnes. Our customers are tire makers, rubber goods producers, cable and optical-fibre jacket makers, and plastics compounders.

## Slide 5: Three Production Bases
Ningbo · Shengzhou
Fangchenggang
3 bases · 350,000 MT/yr in operation
ZHEJIANG
Ningbo
80,000 MT/yr · N330, N326
5 km from Ningbo port
ZHEJIANG
Shengzhou
120,000 MT/yr · N330, N326
Hard-black base; N220, N234 and N375 planned
GUANGXI
Fangchenggang
150,000 MT/yr · N220, N330, N326, N550, N660
35 km to Fangchenggang port · Hanoi 275 km by road
Notes: Here are the three bases. Ningbo, in Zhejiang: 80,000 tonnes a year of N330 and N326, just five kilometres from Ningbo port. Shengzhou, also in Zhejiang: 120,000 tonnes of N330 and N326, with further hard-black grades planned. And Fangchenggang, in Guangxi: our largest base at 150,000 tonnes, making N220, N330, N326, N550 and N660, 35 kilometres from the port and 275 kilometres by road from Hanoi.

## Slide 6: Capacity Roadmap
Chart: Annual capacity by base (thousand MT)
| Ningbo | Shengzhou | Fangchenggang
In operation (2026) | 80 | 120 | 150
Planned total | 80 | 400 | 520
350,000 MT/yr
in operation today (2026)
↓ expanding to
1,000,000 MT/yr
total planned capacity
Planned additions
Shengzhou: N220, N234 and N375 hard blacks, plus a specialty fibre-grade black
Fangchenggang: N774 soft black, plus a specialty conductive black
For you: more grades from one supplier, and multi-base supply of the core grades
Notes: Capacity keeps growing. From 350,000 tonnes a year in operation today, the plan takes total capacity to one million tonnes, mainly at Shengzhou and Fangchenggang. The expansion adds the hard blacks N220, N234 and N375 at Shengzhou, the soft black N774 at Fangchenggang, and specialty fibre-grade and conductive blacks. For customers this means more grades from one supplier and multi-base supply of the core grades.

## Slide 7
02
Why Changhong
Carbon Black
Notes: Now, why Changhong Carbon Black.

## Slide 8: Feedstock & Process
Aromatic-rich oil feedstock
China’s first carbon black producer using aromatic-rich oil. Our process strips feedstock impurities, so heavy metals test as not detected.
Energy recovered on site
Steam and tail gas from the carbon black units replace natural gas and purchased steam in neighbouring plants — lower energy use and lower cost.
A deep petrochemical feedstock pool
China produced about 5 million t of ethylene tar in 2024 and 8–12 million t of FCC slurry oil a year — a broad feedstock base beyond coal tar.
Notes: Three points on feedstock and process. First, we were the first in China to make carbon black from aromatic-rich oil; our process removes feedstock impurities, so heavy metals test as not detected. Second, energy recovery: steam and tail gas from our carbon black units replace natural gas and purchased steam in neighbouring plants, which keeps our energy use and costs down. Third, the feedstock base: China produced around five million tonnes of ethylene tar in 2024 and eight to twelve million tonnes of FCC slurry oil a year, petrochemical feedstocks that broaden supply beyond coal tar.

## Slide 9: Quality Beyond the Standard
Internal controls tighter than China’s national standard and common industry practice
Aromatic-rich-oil feedstock and precise process control give cleaner, more consistent carbon black, with an optimised particle-size distribution under GB/T 3778-2021 for better abrasion resistance.
≤ 300 ppm
45 µm sieve residue
Comparison
National standard ≤ 1,000 ppm
Industry ≤ 500 ppm
≤ 0.8 %
Heating loss
Comparison
National standard ≤ 2.5 %
Industry 2–2.5 %
113 %
N326 tint strength
Comparison
Industry average 108 %
A deeper, purer black
ND
Heavy metals
Comparison
Not detected
COA with every lot
Notes: Our internal controls are tighter than both the national standard and common industry practice. 45-micron sieve residue is controlled within 300 ppm, against a national limit of 1,000 ppm and an industry norm of 500. Heating loss is controlled at 0.8 percent, against 2.5 percent in the national standard. Our N326 reaches 113 percent tint strength, above the 108 percent industry average, which means a deeper, purer black. Heavy metals are not detected, and every lot ships with a COA.

## Slide 10: Sea & Land Logistics
Ningbo base
Zhejiang
5 km
Ningbo port
container terminal
by sea
Worldwide
container routes
Fangchenggang base
Guangxi
by road
Beibu Gulf ports
Fangchenggang (35 km) · Qinzhou
by sea
Southeast Asia
direct sailings
Fangchenggang base
Guangxi
275 km by road
Hanoi
northern Vietnam
For ASEAN buyers
Direct container shipping from the Beibu Gulf to Southeast Asian ports
Overland delivery option to northern Vietnam
Form E / RCEP certificate of origin for preferential duty
Notes: Logistics. Our Ningbo base is five kilometres from Ningbo port, with container routes worldwide. Our Fangchenggang base is 35 kilometres from Fangchenggang port and also ships from Qinzhou, with direct sea freight across Southeast Asia, and it is 275 kilometres by road from Hanoi. ASEAN customers can use a Form E or RCEP certificate of origin for preferential duty rates.

## Slide 11: Industrial-Chain Synergy
For tire makers
Carbon black alongside SSBR and LCBR synthetic rubber for tire compounds from Changhong High-Tech (605008.SH).
80,000 MT/yr SSBR & LCBR
01
For cable & optical-fibre makers
Carbon black supplied together with our PBT and calcium carbonate, for shielded cable and optical-fibre jackets.
300,000 MT/yr PBT
02
Integrated production sites
Every carbon black base runs beside other production units, so by-products are used on site — efficient, lower-cost production.
By-products used on site
03
Notes: Beyond carbon black, the wider Changhong business gives customers a one-stop option. Tire makers can source SSBR and LCBR synthetic rubber from Changhong High-Tech together with our carbon black. Cable and optical-fibre customers can source our PBT and calcium carbonate alongside carbon black for shielded jackets. And because each carbon black base runs next to other production units, by-products are used on site, which keeps production efficient.

## Slide 12
03
Product Portfolio
Notes: Now the product range.

## Slide 13: Grade Map
20
40
60
80
100
120
140
60
70
80
90
100
110
120
130
Iodine adsorption, g/kg → finer particles, more reinforcement
OAN, mL/100 g → higher structure
N220
ISAF · Iodine 121 · OAN 114
N330
HAF · Iodine 82 · OAN 102
N326
HAF-LS · Iodine 82 · OAN 72
N550
FEF · Iodine 43 · OAN 121
N660
GPF · Iodine 36 · OAN 90
Reading the map
→
Right: finer particles and more surface area — more reinforcement and abrasion resistance, more heat build-up.
↑
Up: higher structure — faster extrusion, higher modulus, lower die swell.
●
Hard blacks: treads and reinforcing compounds.
●
Soft blacks: innerliners, carcass and extruded goods.
Plotted at TDS mid-points. ASTM D1765 naming: N = normal cure rate; the first digit is the particle-size group.
Notes: This map places our five core grades by iodine number, which reflects particle size and reinforcement, and by OAN, which reflects structure. Moving right means finer particles: more reinforcement and abrasion resistance, but more heat build-up; that is N220. Moving up means higher structure: faster extrusion and higher modulus; that is N550. N330 sits in the balanced middle, N326 is the low-structure version of N330, and N660 is the coarse, economical soft black.

## Slide 14: Grade N220 · ISAF
N220
ISAF · Intermediate Super Abrasion Furnace
Our highest-reinforcing standard grade — the first choice for tread wear.
Iodine adsorption
121 ± 6 g/kg
OAN
114 ± 6 mL/100 g
COAN
98 ± 6 mL/100 g
Tint strength
116 ± 8 %
Particle size (typical)
20–25 nm
Produced at: Fangchenggang, Guangxi
1
Top-tier reinforcement and abrasion resistance
Fine 20–25 nm particles with about 45 % more surface area than N330 lift abrasion resistance and tensile strength — longer tread life.
2
The balance of wear, heat and processing
Runs cooler and disperses more easily than N110 / N115, and wears far better than N330 — the mainstream tread grade for passenger, truck, bus and OTR tires.
3
High tint, low impurities
Tint 116 ± 8 %, heating loss ≤ 0.8 %, ash ≤ 0.7 %, 45 µm residue ≤ 300 ppm, heavy metals not detected — for goods that need wear resistance and a deep black.
Typical applications
Tire treads
Conveyor-belt covers
Solid tires
Footwear soles
Notes: N220 is the highest-reinforcing grade in our standard range: ISAF under ASTM, produced at our Fangchenggang base. Iodine number around 121 g/kg, OAN around 114, tint strength around 116. Its core value is abrasion resistance: in passenger, truck and OTR tread compounds it gives a clear gain in tread life over N330. Against the finer N110 and N115, it runs cooler and disperses more easily, so it is the practical balance between wear and processing. Beyond tires, it suits conveyor belt covers, solid tires and premium footwear soles that need high wear resistance and a deep black. Our N220 holds heating loss within 0.8 percent, ash within 0.7 percent and 45-micron sieve residue within 300 ppm, heavy metals are not detected, and every lot comes with a COA. If your tread compound already uses N220, we can send samples for a side-by-side trial.

## Slide 15: Grade N330 · HAF
N330
HAF · High Abrasion Furnace
The world’s most widely used reinforcing black — the base grade in almost every formulation.
Iodine adsorption
82 ± 6 g/kg
OAN
102 ± 6 mL/100 g
COAN
88 ± 6 mL/100 g
Tint strength
104 ± 8 %
Particle size (typical)
26–30 nm
Produced at all three bases
1
The all-rounder
Balanced tensile, tear, abrasion and processing: one grade covers tread, carcass, sidewall, conveyor belts, hoses and general rubber goods.
2
Fast to qualify, secure supply
Almost every compounder already runs N330, so a new source qualifies without reformulation. Made at all three of our bases — our most secure supply.
3
Processing-friendly, low impurities
Lower heat build-up and quicker dispersion than N220; heating loss ≤ 0.8 %, ash ≤ 0.7 %, 45 µm residue ≤ 300 ppm, heavy metals not detected — less grit in mixing.
Typical applications
Treads
Carcass & sidewall
Conveyor belts
Hoses
Molded rubber goods
Notes: N330 is the most widely used reinforcing carbon black in the world, HAF under ASTM, and we produce it at all three of our bases. Iodine number around 82 g/kg, OAN around 102, tint around 104. Its strength is balance: good tensile, tear, abrasion and processing all at once, which is why it runs in tread, carcass, sidewall, conveyor belts, hoses and general rubber goods, the base grade in almost every formulation book. For you that means quick qualification with no reformulation. On quality, heating loss is held within 0.8 percent, ash within 0.7 percent and 45-micron sieve residue within 300 ppm, heavy metals are not detected, and every lot comes with a COA. Three bases mean the most secure supply. We quote FOB or CIF to your port. The most direct way to see lot-to-lot consistency is a trial order.

## Slide 16: Grade N550 · FEF
N550
FEF · Fast Extrusion Furnace
The classic fast-extrusion grade — the workhorse for non-tread and extruded goods.
Iodine adsorption
39–47 g/kg
OAN
116–126 mL/100 g
COAN
80–90 mL/100 g
Ash
≤ 0.5 %
Particle size (typical)
40–48 nm
Produced at: Fangchenggang, Guangxi
1
High structure, fast extrusion
OAN 116–126 mL/100 g, the highest structure in our range: fast extrusion, low die swell, a smooth surface and stable dimensions.
2
Low heat build-up, low ash and moisture
Coarser particles mean lower compound viscosity, lower hysteresis and good flex-fatigue life; heating loss ≤ 0.8 %, ash ≤ 0.5 %, 45 µm residue ≤ 300 ppm.
3
Cost-efficient and close to Southeast Asia
Takes high loadings while keeping flow. Ships 35 km to the port for direct sea freight across Southeast Asia.
Typical applications
Innerliners
Sidewalls & carcass
Hoses
Seals & profiles
Cable sheathing
Anti-vibration parts
Notes: N550 is the classic fast-extrusion grade among semi-reinforcing blacks, FEF under ASTM, produced at our Fangchenggang base in Guangxi. Iodine number around 43 g/kg, OAN around 121, the highest structure in our range. The high structure pays off in processing: fast extrusion, low die swell, smooth extrudate and stable dimensions. The coarser particle and low surface area pay off in performance: low heat build-up, low compound viscosity and good flex life, with heating loss held within 0.8 percent and ash within 0.5 percent. That is why it goes into tire innerliners, sidewalls and carcass, and into hoses, seals, cable sheathing and anti-vibration parts. It takes high loadings, so compounds stay cost-efficient. Fangchenggang is 35 kilometres from the port, so containers ship by sea straight to Southeast Asia, and ASEAN customers can claim preferential duty. COA with every lot, quoted FOB or CIF.

## Slide 17: Completing the Range: N326 & N660
N326
HAF-LS · low-structure HAF
Iodine adsorption
82 ± 6 g/kg
OAN
72 ± 6 mL/100 g
COAN
68 ± 6 mL/100 g
Tint strength
111 ± 8 %
113 % tint strength — above the 108 % industry average
Low structure gives high tensile and tear strength at a lower modulus: steel-cord skim and bead compounds, plus general rubber goods.
Produced at all three bases
N660
GPF · General Purpose Furnace
Iodine adsorption
32–40 g/kg
OAN
85–95 mL/100 g
COAN
69–79 mL/100 g
pH
6.0–10.0
N550 for extrusion precision; N660 for cost and low heat build-up
Coarser particles (typically 49–60 nm) give lower heat build-up, higher loadings and lower cost than N550: innerliners, carcass, hoses, seals and extruded profiles.
Produced at: Fangchenggang, Guangxi
Notes: Two more grades complete the core range. N326 is a low-structure HAF: with OAN around 72 it gives high tensile and tear strength at a lower modulus, which suits steel-cord skim and bead compounds; our N326 reaches 113 percent tint strength, against a 108 percent industry average. N660 is the general-purpose soft black: coarser than N550, with lower heat build-up, higher loadings and lower cost, for innerliners, carcass, hoses, seals and profiles. A simple rule: N550 for extrusion precision, N660 for cost and low heat build-up.

## Slide 18: Grade Selection Guide
 | Application | N220 | N330 | N326 | N550 | N660
Tires | Tread | ● | ○ |  |  | 
 | Sidewall |  | ● |  | ● | ○
 | Carcass / ply |  | ● |  | ● | ●
 | Innerliner |  |  |  | ● | ●
 | Steel-cord skim & bead |  |  | ● |  | 
Rubber goods | Conveyor-belt covers | ● | ● |  |  | 
 | Hoses |  | ○ |  | ● | ●
 | Seals & extruded profiles |  |  |  | ● | ●
 | Cable sheathing |  |  |  | ● | 
 | Anti-vibration parts |  | ○ |  | ● | 
 | Footwear soles | ● | ○ |  |  | 
● Recommended ○ Also used Final choice depends on your compound and process — we are glad to review your current formulation.
Notes: This guide summarises where each grade fits. The first question is always which compound or tire component it is for. Treads call for N220; carcass and sidewall for N330 and N550; innerliners for N550 and N660; steel-cord skim and bead compounds for N326. The final choice depends on your compound and process, and we are glad to review your current formulation.

## Slide 19: Technical Data Sheet
Property | Unit | N220 | N330 | N326 | N550 | N660 | Test method
Iodine adsorption | g/kg | 121 ± 6 | 82 ± 6 | 82 ± 6 | 39–47 | 32–40 | GB/T 3780.1-2015
Oil absorption (OAN) | mL/100 g | 114 ± 6 | 102 ± 6 | 72 ± 6 | 116–126 | 85–95 | GB/T 3780.2-2017
Compressed OAN (COAN) | mL/100 g | 98 ± 6 | 88 ± 6 | 68 ± 6 | 80–90 | 69–79 | GB/T 3780.4-2017
Tint strength | % | 116 ± 8 | 104 ± 8 | 111 ± 8 | — | — | GB/T 3780.6-2016
Heating loss (125 °C, 1 h) | % | ≤ 0.8 | ≤ 0.8 | ≤ 0.8 | ≤ 0.8 | ≤ 0.8 | GB/T 3780.8-2019
Ash content | % | ≤ 0.7 | ≤ 0.7 | ≤ 0.7 | ≤ 0.5 | ≤ 0.5 | GB/T 3780.10-2017
45 µm sieve residue | ppm | ≤ 300 | ≤ 300 | ≤ 300 | ≤ 300 | ≤ 300 | GB/T 3780.21-2016
Fines content | % | ≤ 7.0 | ≤ 7.0 | ≤ 7.0 | ≤ 10.0 | ≤ 7.0 | GB/T 14853.2-2016
Pellet hardness | cN | 30 ± 10 | 30 ± 10 | 30 ± 10 | — | — | GB/T 14853.6-2013
pH | — | 5.0–9.0 | 5.0–9.0 | 5.0–9.0 | 5.0–9.0 | 6.0–10.0 | GB/T 3780.7-2016
Pour density | kg/m³ | 355 ± 40 | 380 ± 40 | 455 ± 40 | 320–400 | 400–480 | GB/T 14853.1-2013
Product specifications of Zhejiang Changhong Biological Material Co., Ltd. OAN and COAN in mL/100 g (= 10⁻⁵ m³/kg). Packing: 25 kg bags; 500 kg and 1,000 kg jumbo bags.
Notes: Here is the technical data sheet for our five core grades, with Chinese GB/T test methods. If you ask for ASTM equivalents: iodine D1510, OAN D2414, COAN D3493, tint D3265, heating loss D1509, ash D1506, sieve residue D1514, fines D1508, pellet hardness D5230, pH D1512 and pour density D1513. Packing is 25 kg bags or 500 and 1,000 kg jumbo bags.

## Slide 20
04
Working With Us
Notes: Finally, how we can work together.

## Slide 21: From Sample to Supply
01
Grade match
Share your current grade, compound and specification; we propose the matching grade with our TDS and recent COA data.
02
Samples & lab test
Samples with a COA for lab evaluation and a side-by-side comparison with your current black.
03
Trial order
A trial lot in production confirms lot-to-lot consistency before volumes grow.
04
Regular supply
Scheduled container shipments from Ningbo or the Beibu Gulf, with a COA for every lot.
Commercial terms
Packing
25 kg bags; 500 / 1,000 kg jumbo bags
Incoterms
FOB · CFR · CIF
Payment
T/T or L/C, subject to credit approval
Documents
COA per lot · TDS · Form E / RCEP C/O · HS 2803.00
Notes: Starting is simple. Share your current grade, compound and specification, and we propose the matching grade with our TDS and recent COA data. We then send samples with a COA for lab evaluation and a side-by-side comparison. A trial order confirms lot-to-lot consistency in production, and then we move to regular container shipments from Ningbo or the Beibu Gulf, with a COA for every lot. We pack in 25 kg bags or 500 and 1,000 kg jumbo bags, quote FOB, CFR or CIF, and accept T/T or L/C subject to credit approval.

## Slide 22
CHANGHONG
Thank you
Xuzhe (Batiste) Gao
Marketing Division II / Carbon Black
Keyuan Holding Group Co., Ltd.
ZHEJIANG CHANGHONG BIOLOGICAL MATERIAL CO., LTD.
Work Email: gaoxz@kygroup.ltd
Personal Email: ish566002@gmail.com
WhatsApp: +44 7536 287291
Mobile: +86 15990233826
Notes: Thank you. I am happy to take your questions. My contact details are on this slide; email or WhatsApp both work.